Development of Thermal Insulated Structural Concrete and Its Mechanical Strength Using Different

Table 1: Physical properties of Light weight aggregates

| Aggregate ID | Shape & Size in mm | Bulk density | Water absorption (%) | Specific gravity | Impact value |
| --- | --- | --- | --- | --- | --- |
| Micron ball | Spherical (0-20) | 800 | 15.66 | 1.71 | 29.65 |
| Sintered fly ash | Spherical (10-20) | 800 | 22 | 1.75 | 44.75 |

Table 2: Chemical properties of micron ball aggregates

| Composition | Loss of Ignition (%) | Silicon Dioxide (%) | Aluminium Oxide (Al2O3) (%) | Ferric Oxide (Fe2O3) (%) | Calcium Oxide (CaO) (%) | Magnesium Oxide (MaO) (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Micron Ball | 2 | 79.1 | 4.2 | 1.3 | 8 | 1.2 |

| Materials | Cement (kg/m3) | Fly ash (kg/m3) | Sand (kg/m3) | SFA (kg/m3) | MB (kg/m3) | Natural Aggregate (kg/m3) | Water(li) | Admixture (kg/m3) | PP Fiber (kg/m3) | Total (kg/m3) (Theoretical density) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mix-1(M30) | 318 |  | 673 | - | - | 1290 | 177 | 2.226 | - | 2460.2 |
| Mix-2 | 418 | 451 | 343 | 345 | - | - | 309 | 3.3 | 1 | 1870.3 |
| Mix-3 | 418 | 451 | 343 | - | 345 | - | 287.4 | 3.3 | - | 1847.7 |

Table: 3 Mix proportions of developed concrete

Table: 4 Compressive strength

| Mix designs | 7 DAYS (MPa) | 28DAYS(MPa) |
| --- | --- | --- |
| Mix 1 | 32 | 37 |
| Mix 2 | 20 | 25 |
| Mix 3 | 31 | 43 |

Table: 5 Flexural strength strength

| Mix designs | Flexural strength at 7 days | Flexural strength at 28 days |
| --- | --- | --- |
| Mix 1 | 2.8 | 3.8 |
| Mix 2 | 2.6 | 3.35 |
| Mix 3 | 2.7 | 4.11 |

Table: 6 Tensile Strength of concrete

| Mix designs | Tensile Strength of concrete 28 days (MPa) |
| --- | --- |
| Mix 1 | 1.6 |
| Mix 2 | 1.3 |
| Mix 3 | 2.4 |

Table: 6 Thermal insulation of concrete

| Mix designs | Thermal insulation of concrete (W/m.K) |
| --- | --- |
| Mix 1 | 0.819 |
| Mix 2 | 0.543 |
| Mix 3 | 0.321 |